[image: image1.jpg]






                             

                   [image: image2.jpg]




Product: AL Complex Graphite EP 0, 00  


	Sr.No.
	Test
	EP0 Typical 


	EP00

Typical
	Test Method

	1
	Penetration:
	
	
	ASTM D 217-02

	
	 Work 60X
	355 – 385
	400 – 430
	

	
	Typical
	370
	415
	

	2
	NLGI Grade
	0
	00
	

	3
	Drop Point ((C)
	>195
	 >180
	ASTM D 566

	4
	Appearance
	Silvery Black
	Silvery Black
	Visual

	5
	Soap Type
	Aluminium Complex 
	Aluminium Complex 
	

	6
	Base oil Viscosity* (KV@40(C),cSt
	1000 - 1200
	2500 - 3000
	ASTM D 445

	
	Base Oil Type
	Semi-Synthetic
	Semi-Synthetic
	

	7
	Copper corrosion
	1b Max
	 1b Max
	ASTM D 4048

	8
	4 Ball Weld Load (Kg)
	620
	800
	ASTM D 2596

	9
	4 Ball Wear Scar (mm)
	0.5 Max
	0.5 Max
	ASTM D 2266

	10
	Graphite (%)
	8
	8
	


                      
          Product Data                       

· - Can be made to customers desired spec    

   TURBHE CHEMICALS PVT. LTD.









