[image: image1.jpg]






                             

                   [image: image2.jpg]




 

         PRODUCT DATA SHEET


                 Calcium Complex Grease

 Calcium Complex greases are Calcium soap thickened greases which have been complexed using a complexing agent. This complexing improves the performance of the grease, especially the high temperature performance.
 These greases have a durable film & good pumpability. 

These greases are used mainly in automotive undercarriage applications & also in industrial applications requiring high temperature capability.

  These greases are suitable for applications with an operating temperature range of -10 to +180 0C under routine service. 

Applications

· Automotive undercarriage

· Farm equipment

· Mining & Crushing equipment

· Cement & Steel mills

Main Benefits

· Excellent resistance to water washout

· Good for use in harsh, high temperature environments

· Superior boundary film strength leading to reduction in maintenance costs and downtime

Product:  Calcium Complex Greases  
                      
           Product Data                             

	Sr.No.
	Test
	Calcium Complex 3 
	Calcium Complex EP2
	Test Method

	1
	Penetration:
	
	
	ASTM D 217-02 

	
	 Work 60X
	220 - 250
	265 - 295
	

	
	Typical
	235
	280
	

	2
	NLGI Grade
	3
	2
	

	3
	Drop Point ((C)
	>240
	 >240
	     ASTM D 566

	4
	Colour
	Brown
	Brown
	Visual

	5
	Soap Type
	Calcium Complex
	Calcium Complex
	

	6
	Base oil Viscosity (KV@40(C),cSt
	120 – 140
	120 - 140
	ASTM D 445

	7
	Base Oil Type
	Mineral
	Mineral
	

	8
	Resistance to water washout (% loss)
	<4
	<5
	ASTM D 1264

	9
	Oxidation Stability 

100 hrs @ 100C, drop in pressure, Psi
	<5
	<5
	ASTM D 942

	10
	Copper corrosion
	1b Max
	 1b Max
	ASTM D 4048

	11
	4 Ball Weld Load (Kg)
	-
	250
	    ASTM D 2596












Page 2 of 2

   TURBHE CHEMICALS PVT. LTD.









