[image: image1.jpg]






                             

                   [image: image2.jpg]




                     PRODUCT DATA SHEET


           Cable & Wire Rope Greases
Cable & Wire Rope greases, formulated & designed to coat wire ropes, moving chains &cable parts.

Our Wire Rope greases are manufactured under strictly controlled conditions using premium quality base oils & are fortified with corrosion & oxidation inhibitors, anti-wear & tackiness additives. They are formulated to be tacky & reduce water washout, corrosion & wear. 

 These products are supplied in NLGI 0, 00 & 000 consistencies.

. 

Applications

· Wire ropes

· Cables

· Moving chains (links, pins & bushings)

Main Benefits

· Excellent wear reduction

· Superior Oxidation & Heat stability

· Superior boundary film strength leading to reduction in maintenance costs and downtime
· Superior resistance to water washout
· Superior Roll & Shear stability

· Excellent as a sealing agent (for repelling moisture)
· Superior protection against rust and corrosion
Product: Lithium - Calcium 0, 00, 000
	Sr.No.
	Test
	EP0 Typical 


	EP00

Typical
	EP000

Typical
	Test Method

	1
	Penetration:
	
	
	
	ASTM D 217-02

	
	 Work 60X
	355 – 385
	400 – 430
	445 – 475
	

	
	Typical
	370
	415
	460
	

	2
	NLGI Grade
	0
	00
	000
	

	3
	Appearance
	Brown, smi-fluid, tacky
	Brown, smi-fluid, tacky
	Brown, smi-fluid, tacky
	Visual

	4
	Soap Type
	Lithium - Calcium 
	Lithium - Calcium 
	Lithium - Calcium 
	

	5
	Base oil Viscosity (KV@40(C),cSt
	100 - 120
	100 - 120
	100 - 120
	ASTM D 445

	6
	Base Oil Type
	Mineral
	Mineral
	Mineral
	

	7
	Copper corrosion
	1b Max
	 1b Max
	 1b Max
	ASTM D 4048

	8
	4 Ball Weld Load (Kg)
	250
	250
	250
	ASTM D 2596

	9
	Corrosion Prevention
	Pass
	Pass
	Pass
	ASTM D 1743


   
     Typical Performance Data                       

Product: Lithium Complex MOLY 0, 00, 000

	Sr.No.
	Test
	EP0 Typical 


	EP00

Typical
	EP000

Typical
	Test Method

	1
	Penetration:
	
	
	
	ASTM D 217-02

	
	 Work 60X
	355 – 385
	400 – 430
	445 – 475
	

	
	Typical
	370
	415
	460
	

	2
	NLGI Grade
	0
	00
	000
	

	3
	Appearance
	Silvery Black, semi-fluid, tacky
	Silvery Black, semi-fluid, tacky
	Silvery Black, semi-fluid, tacky
	Visual

	4
	Soap Type
	Lithium Complex
	Lithium Complex 
	Lithium Complex 
	

	5
	Base oil Viscosity (KV@40(C),cSt
	100 - 120
	100 - 120
	100 - 120
	ASTM D 445

	6
	Base Oil Type
	Mineral
	Mineral
	Mineral
	

	7
	Copper corrosion
	1b Max
	 1b Max
	 1b Max
	ASTM D 4048

	8
	4 Ball Weld Load (Kg)
	250
	250
	250
	ASTM D 2596

	9
	Corrosion Prevention
	Pass
	Pass
	Pass
	ASTM D 1743

	10
	MOLY (%)
	3
	3
	3
	


   
     Typical Performance Data                       









         
  Page 3 of 3

   TURBHE CHEMICALS PVT. LTD.









