[image: image1.jpg]






                             

                   [image: image2.jpg]




                     PRODUCT DATA SHEET


          Lithium Complex 80K Grease

This is a Lithium Complex soap based, premium quality multipurpose grease. It is manufactured under strictly controlled conditions using premium quality base oils & is fortified with extreme pressure (EP) additives & corrosion & oxidation inhibitors. 

 This product has a durable film & superior surface adhesion. This grease also has good shear stability & good roll stability making it a very versatile solution, with a wide variety of potential applications.  

  This grease is suitable for applications with an operating temperature range of
 -20 to +180 0C under routine service. 

This product can be recommended for a service life of 80,000 Km

Applications

· Automotive wheel bearings, chassis, steering components etc.

· Earthmoving, mining and quarrying equipment under moderate to heavy loads

· Farm equipment like tractors, harvesters, implements etc

· Universal joints bearings, journal bearings etc

Main Benefits

· Excellent Oxidation & Heat stability

· Superior boundary film strength leading to reduction in maintenance costs and downtime

· Superior resistance to water washout

· Superior Roll & Shear stability

· Excellent retention of structure under extreme operating conditions and under storage

· Superior protection against rust and corrosion

Performance standards

Exceeds the performance requirements of 

· IS 12203

Product: Lithium Complex 80K           
                     Typical Performance Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Penetration:
	
	
	ASTM D 217-02 

	
	 Work 60X
	220 – 250
	234
	

	
	Work 100,000X
	+30
	+25
	

	2
	NLGI Grade
	3
	3
	

	3
	Drop Point ((C)
	>240
	 >250
	     ASTM D 566

	4
	EMCOR  Rust Prevention
	0-0 Pass
	0-0 Pass
	IP 220/93

	5
	Appearance
	Light Brown
	Light Brown
	Visual

	6
	Soap Type
	Lithium Complex
	Lithium Complex
	

	7
	Base oil Viscosity (KV@40(C),cSt
	200 - 220
	210
	ASTM D 445

	
	Base Oil Type
	Mineral
	Mineral
	

	8
	Oil separation

 40(C for 168 Hrs (% loss)
	5 Max
	<1.5
	IS 1448

	9
	Resistance to water washout (% loss)
	10 Max
	<4
	ASTM D 1264

	10
	Oxidation Stability 

100 hrs @ 100C, drop in pressure, Psi
	6 Max
	<4
	ASTM D 942

	11
	Copper corrosion
	1b Max
	 1b
	ASTM D 4048

	12
	4 Ball Weld Load (Kg)
	315 Min
	315
	    ASTM D 2596

	13
	4 Ball Wear Scar mm
	0.6 Max
	0.4
	    ASTM D 2266

	14
	Wheel bearing Life 
	60 Hours Min
	>100
	ASTM D 3527

	15
	Roll Stability

16 Hours @80℃
	25 Max
	<20
	ASTM D 1831

	16
	Wheel bearing Test
	Max 5 g
	<0.2
	ASTM D 1263

	17
	Temperature Range (℃)
	-20 to +180
	-20 to +180
	












Page 2 of 2

   TURBHE CHEMICALS PVT. LTD.









