[image: image1.jpg]






                      

                               [image: image2.jpg]




Product: Multigrade Engine Oil SAE 15W 40  


                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	4.0 max.
	3.5
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.881
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	14.0 - 15.5
	15.0
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	Report
	116.5
	ASTM D 445

	6
	Viscosity Index
	130 min.
	133
	ASTM D 2270

	7
	TBN, mg KOH/gm
	10.5 min.
	10.8
	ASTM D 2896

	8
	Flash Point, (C
	220 min.
	224
	ASTM D 92

	9
	Pour Point, (C
	-24 max.
	-24
	ASTM D 97

	10
	CCS @-20(C, mPa.s
	7000 max.
	6600
	ASTM D 5293


   TURBHE CHEMICALS PVT. LTD.








