[image: image1.jpg]






                      

                               [image: image2.jpg]




   
      Product: Hydraulic HVI 68  


                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	2.5 max.
	L 2.5
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8830
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	Report
	10.90
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	64.0 - 72.0
	67.20
	ASTM D 445

	6
	Viscosity Index
	150 min.
	153
	ASTM D 2270

	7
	Flash Point, (C
	210 min.
	212
	ASTM D 92

	8
	Pour Point, (C
	-12 max.
	-12
	ASTM D 97


   TURBHE CHEMICALS PVT. LTD.








