[image: image1.jpg]






                      

                               [image: image2.jpg]




   
    Product: Soluble Cutting Oil  


                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	Dark Amber
	Dark Amber
	Visual

	3
	Density @29.5(C, gm/ml
	Report
	0.9000
	ASTM D 1298

	4
	Kin. Vis. @40(C, cSt
	30.0 - 55.0
	34
	ASTM D 445

	5
	Flash Point, (C
	150 min.
	155
	ASTM D 92

	6
	Pour Point, (C
	0 max.
	-6
	ASTM D 97

	7
	Cast Iron Corrosion (20:1 Emulsion 800 ppm) 
	0 / 0-1
	Passes
	IS: 1115

	8
	Emulsion Stability 24 hours in 500 ppm water & frothing Test  
	Passes
	No oil layer, no cream formation
	IS: 1115

	9
	Thermal Stability Test
	Passes
	Passes
	IS: 1115

	10
	5% emulsion PH in Distilled water
	8.5 min.
	9.10
	IS: 1115


   TURBHE CHEMICALS PVT. LTD.








