[image: image1.jpg]






                      

                               [image: image2.jpg]




Product: CNG SAE 20W 50

CLASS: API SF / CD

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	Dyed Red
	Dyed Red
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8842
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	18.5 - 20.5
	19.5
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	Report
	185.5
	ASTM D 445

	6
	Viscosity Index
	120 min.
	120
	ASTM D 2270

	7
	TBN, mg of KOH/gm
	5.3 min.
	5.4
	ASTM D 2896

	8
	Flash Point, (C
	230 min.
	234
	ASTM D 92

	9
	Pour Point, (C
	-21 max.
	-21
	ASTM D 97

	 10
	CCS @-15(C, mPa.s
	9500 max.
	9250
	ASTM D 5293

















   TURBHE CHEMICALS PVT. LTD.








