[image: image1.jpg]






                      

                               [image: image2.jpg]




      Product: Pump Set Oil SAE 40  

CLASS: API CC / SC,  IS:13656:2002 TYPE E-DL1, EPL-1, MIL-L-2104 B

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	Dyed Red
	Dyed Red
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8840
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	14.0  - 15.5
	14.5
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	Report
	133.6
	ASTM D 445

	6
	Viscosity Index
	98 min.
	105
	ASTM D 2270

	7
	TBN, mg of KOH/gm
	4.5 min.
	4.7
	ASTM D 2896

	8
	Flash Point, (C
	220 min.
	230
	ASTM D 92

	9
	Pour Point, (C
	-9 max.
	-9
	ASTM D 97














   TURBHE CHEMICALS PVT. LTD.











