[image: image1.jpg]






                      

                               [image: image2.jpg]




   

    Product: Gear 80W 90

CLASS: API GL4, MIL-L-2105, IS 1118 : 1992

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	3.5 max.
	2.5
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8890
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	14.5 - 15.5
	15.0
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	Report
	155.1
	ASTM D 445

	6
	Viscosity Index
	95 min.
	96
	ASTM D 2270

	7
	TAN, mg of KOH/gm
	Report
	0.9
	ASTM D 664

	8
	Flash Point, (C
	220 min.
	230
	ASTM D 92

	9
	Pour Point, (C
	-21 max.
	-21
	ASTM D 97

















   TURBHE CHEMICALS PVT. LTD.








