[image: image1.jpg]






                      

                               [image: image2.jpg]




  Product: Gear Oil 90 SP  

CLASS: API GL 5, MIL-L-2105, IS 1118:1992
Product Data
	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	3.5 max.
	2.5
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8890
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	17.0 - 19.0
	18.2
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	Report
	220.1
	ASTM D 445

	6
	Viscosity Index
	90 min.
	90
	ASTM D 2270

	7
	TAN, mg of KOH/gm
	Report
	1.7
	ASTM D 664

	8
	Flash Point, (C
	220 min.
	228
	ASTM D 92

	9
	Pour Point, (C
	-9 max.
	-12
	ASTM D 97

















   TURBHE CHEMICALS PVT. LTD.








