[image: image1.jpg]






                      

                               [image: image2.jpg]




Product: Industrial Gear 220

CLASS: AGMA 250.04, US STEEL 222&224, IS 8406-93, DIN 51517.3

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	4.5 max.
	3.0
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8890
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	Report
	18.8
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	210 - 240
	220.0
	ASTM D 445

	6
	Viscosity Index
	90 min.
	95
	ASTM D 2270

	7
	TAN, mg of KOH/gm
	Report
	0.6
	ASTM D 664

	8
	Flash Point, (C
	230 min.
	236
	ASTM D 92

	9
	Pour Point, (C
	-9 max.
	-12
	ASTM D 97

















   TURBHE CHEMICALS PVT. LTD.








