[image: image1.jpg]






                      

                               [image: image2.jpg]




   

   Product: Quenching Oil  

CLASS: ANTIOXIDENT MEDIUM GRADE For  COLDQUENCHING SYSTEM

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	3.0 max.
	1.5
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8650
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	Report
	5.2
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	28.0 – 34.0
	30.4
	ASTM D 445

	6
	Viscosity Index
	90 min.
	100
	ASTM D 2270

	7
	TAN, mg of KOH/gm
	Report
	0.6
	ASTM D 664

	8
	Flash Point, (C
	190 min.
	204
	ASTM D 92

	9
	Pour Point, (C
	-3 max.
	-6
	ASTM D 97

















   TURBHE CHEMICALS PVT. LTD.








