[image: image1.jpg]






                      

                               [image: image2.jpg]




Product: Transmission Oil 4 10  

CLASS: C 4 OF ALLISON TRANSMISSION DIVISION OF G.M. USA

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	2.0 max.
	1.5
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8760
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	6.0 - 7.0
	6.56
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	35.0 - 40.0
	39.80
	ASTM D 445

	6
	Viscosity Index
	95 min.
	117
	ASTM D 2270

	7
	Flash Point, (C
	210 min.
	220
	ASTM D 92

	8
	Pour Point, (C
	-21 max.
	-24
	ASTM D 97

	9
	TAN, mg of KOH/gm
	Report
	2.45
	ASTM D 664

	 10
	TBN, mg of KOH/gm
	8.0 min.
	8.2
	ASTM D 2896

















   TURBHE CHEMICALS PVT. LTD.








