[image: image1.jpg]






                      

                               [image: image2.jpg]




   Product: Transmission Oil 4 30  

CLASS: C 4 OF ALLISON TRANSMISSION DIVISION OF G.M. USA

                      
           Product Data                             

	Sr.No.
	Test
	Control Range / Limit 
	Typical
	Test Method

	1
	Appearance
	Clear & Bright Oil
	Clear & Bright Oil
	Visual

	2
	Colour
	3.5 max.
	3.0
	ASTM D 1500

	3
	Density @29.5(C, gm/ml
	Report
	0.8868
	ASTM D 1298

	4
	Kin. Vis. @100(C, cSt
	10.0 – 12.5
	11.25
	ASTM D 445

	5
	Kin. Vis. @40(C, cSt
	90.0 min.
	95.20
	ASTM D 445

	6
	Viscosity Index
	95 min.
	104
	ASTM D 2270

	7
	Flash Point, (C
	220 min.
	226
	ASTM D 92

	8
	Pour Point, (C
	-18 max.
	-21
	ASTM D 97

	9
	TAN, mg of KOH/gm
	Report
	2.60
	ASTM D 664

	 10
	TBN, mg of KOH/gm
	8.0 min.
	8.2
	ASTM D 2896

















   TURBHE CHEMICALS PVT. LTD.








