[image: image1.jpg]






                             

                   [image: image2.jpg]




 

         PRODUCT DATA SHEET


                  Bentonite Clay Grease   
 Bentonite greases are non-soap, inorganic clay thickened greases. These are non-melt greases and are therefore typically used in harsh industrial applications requiring lubrication under very high temperatures. These greases are typically used in plain & roller bearings operating at temperatures at which conventional soap thickened greases cannot work.These greases have a durable film & good pumpability. 

These greases are suitable for applications with an operating temperature range of -10 to +200 0C under routine service. 

Applications

· Bearings in Sugar Mills operating at very high temperatures

· Plastic injection moulding

Main Benefits

· Excellent in very high temperature applications where conventional soap greases cannot be used

· Non-melt

· Superior boundary film strength leading to reduction in maintenance costs and downtime
· Good resistance to water washout
· Superior Roll & Shear stability

· Good EP properties especially when combined with MOLY
· Superior protection against rust and corrosion
Product:  Bentonite Clay Grease

                 Typical Performance Data                             

	Sr.No.
	Test
	Bentone Clay 2 
	Bentone Clay 2 MOLY
	Test Method

	1
	Penetration:
	
	
	ASTM D 217-02 

	
	 Work 60X
	265 - 295
	265 - 295
	

	2
	NLGI Grade
	285
	285
	

	3
	Drop Point ((C)
	>260
	 >260
	     ASTM D 566

	5
	Appearance
	Light Brown
	Silvery - Black
	Visual

	6
	Soap Type
	Non-Soap
	Non-Soap
	

	7
	Base oil Viscosity (KV@40(C),cSt
	380 - 420
	1200 - 1400
	ASTM D 445

	
	Base Oil Type
	Mineral
	Semi-Synthetic
	

	8
	Oil separation

 100(C for 30 Hrs (% loss)
	2 Max
	2 Max
	IS 1448

	9
	Resistance to water washout (% loss)
	<10 
	<5
	ASTM D 1264

	10
	Oxidation Stability 

100 hrs @ 100C, drop in pressure, Psi
	<5
	<5
	ASTM D 942

	11
	Copper corrosion
	1b Max
	 1b Max
	ASTM D 4048

	12
	4 Ball Weld Load (Kg)
	-
	250
	    ASTM D 2596

	13
	MOLY (%)
	-
	3
	












Page 2 of 2

   TURBHE CHEMICALS PVT. LTD.









