[image: image1.jpg]






                                                                           [image: image2.jpg]



                          


	Sr.No.
	Test
	Results
	Test Method

	1
	Penetration:
	
	ASTM D 217-02

	
	Work 60X
	280
	

	2
	NLGI Grade
	2
	

	3
	Drop Point ((C)
	>275
	ASTM D 566

	4
	Colour
	Dark Brown
	

	5
	Thickener type
	Calcium Sulfonate
	

	6
	Base oil Viscosity (KV@40(C), cSt
	>220
	ASTM D 445

	7
	Oil separation
 100(C for 30 Hrs
 (% loss)
	<5
	IS 1448 [P:84]

	8
	4 Ball Weld Load (Kg)
	> 315
	ASTM D 2596


  TURBHE CHEMICALS  PVT. LTD.                          





 Typical Performance Data: Calcium Sulfonate Complex 2 Grease 









