[image: image1.jpg]






                                                     [image: image2.jpg]




                       PRODUCT DATA SHEET


                     Lithium AP Greases

  These are Lithium soap based, premium quality multipurpose greases. They are manufactured under strictly controlled conditions using premium quality base oils & is fortified with rust & oxidation inhibitors. 

 These products have a durable film & good surface adhesion. These greases also have good shear stability & good roll stability making them versatile & cost effective greasing solutions, with a wide variety of potential applications.  

  They are suitable for applications with an operating temperature range of -20 to +120 0C under routine service. 

Applications

· Automotive wheel bearings, chassis, steering components etc.

· Earthmoving, mining and quarrying equipment under moderate 

· Farm equipment like tractors, harvesters, implements etc

· Water pumps, generators, universal joints bearings, journal bearings etc

Main Benefits

· Excellent Oxidation & Heat stability

· Superior boundary film strength leading to reduction in maintenance costs and downtime

· Superior resistance to water washout

· Superior Roll & Shear stability

· Excellent retention of structure under extreme operating conditions and under storage

· Superior protection against rust and corrosion

Performance standards

Exceeds the performance requirements of 

· IS 7623


             Product: Lithium AP3, AP2

                    TC-AP3, AP2 

                  Typical Performance Data                             

	Sr.No.
	Test
	AP3 

Typical Range / Limit 
	AP2 

Typical Range / Limit
	Test Method

	1
	Penetration:
	
	
	ASTM D 217-02 

	
	Range
	220 - 250
	265 - 205
	

	
	 Work 60X
	235
	280
	

	
	Work 100,000X
	+30
	+25
	

	2
	NLGI Grade
	3
	2
	

	3
	Drop Point ((C)
	>190
	 >190
	     ASTM D 566

	4
	EMCOR  Rust Prevention
	0-0 Pass
	0-0 Pass
	IP 220/93

	5
	Colour
	Light Brown
	Light Brown
	Visual

	6
	Soap Type
	Lithium
	Lithium
	

	7
	Base oil Viscosity (KV@40(C),cSt
	100 - 120
	100 - 120
	ASTM D 445

	
	Base Oil Type
	Mineral
	Mineral
	

	8
	Oil separation

 100(C for 30 Hrs (% loss)
	<2
	<5
	IS 1448

	9
	Resistance to water washout (% loss)
	4 Max
	5 Max
	ASTM D 1264

	10
	Oxidation Stability 

100 hrs @ 100C, drop in pressure, Psi
	5 Max
	5 Max
	ASTM D 942

	11
	Copper corrosion
	1b Max
	 1b Max
	ASTM D 4048

	12
	Roll Stability

16 Hours 
	25 Max
	25 Max
	ASTM D 1831

	13
	Wheel bearing Test (g)
	1 Max
	2 Max
	ASTM D 1263

	14
	Operating Range ((C)
	-20 to +120
	-20 to +120
	


                                                                                                                                                        Page 2 of 2

    TURBHE CHEMICALS PVT. LTD.









