[image: image1.jpg]






                                                          [image: image2.jpg]




                           PRODUCT DATA SHEET


                   Lithium EP Greases
  These are Lithium soap based, premium quality EP/multipurpose greases. They are manufactured under strictly controlled conditions using premium quality base oils & is fortified with EP additives and rust & oxidation inhibitors. 

 This range of products have very durable film & superior surface adhesion. These greases also have good shear stability & good roll stability making them very versatile greases, with a wide variety of potential applications. This range of Lithium EP greases have been designed to handle medium to heavy loads for extended periods & also the occasional shock loading. 

  They are suitable for applications wherein operating temperatures rise up to 130 0C under routine service. The consistency & excellent pumpability of these products also make them suitable for centralized lubrication systems. 

  Lithium EP greases have been designed, engineered & formulated to provide robust EP capability at the boundary film level, superior pumpability & heat stability, & therefore, longer service life. Their operating temperature range is -20℃ to + 130℃.
Applications

· Automotive wheel bearings, chassis, steering components etc.

· Earthmoving, mining and quarrying equipment under moderate 

· Farm equipment like tractors, harvesters, implements etc

· Water pumps, generators, universal joints bearings, journal bearings etc

Main Benefits

· Excellent Oxidation & Heat stability

· Superior boundary film strength leading to reduction in maintenance costs and downtime
· Superior resistance to water washout
· Superior Roll & Shear stability

· Excellent retention of structure under extreme operating conditions and under storage
· Superior protection against rust and corrosion
Performance standards

Exceeds the performance requirements of 

· IS 7623

                     Typical Performance Data 
                  Lithium EP Greases NLGI 3, 2 
	Sr.No.
	Test
	Control Range/Limit

EP3
	Control Range/Limit

EP2
	Control Range/Limit

EP2+
	Test Method

	1
	Penetration:
	
	
	
	ASTM D 217-02

	
	 Work 60X
	220 – 250
	265 – 295
	265 – 295
	

	
	Typical
	235
	280
	280
	

	2
	Work 100,000X
	+30 Max 

(from Work 60X)
	+30 Max 

(from Work 60X)
	+30 Max

(from Work 60X)
	ASTM D 217

	3
	NLGI Grade
	3
	2
	2
	

	4
	Drop Point ((C)
	>180
	>180
	>180
	ASTM D 566

	5
	  Rust Preventive Characteristic
	Pass
	Pass
	Pass
	ASTM D 1743

	6
	Colour
	Golden Brown
	Golden Brown
	Golden Brown
	Visual

	7
	Soap
	Lithium
	Lithium
	Lithium
	

	8
	Appearance
	Smooth, Buttery & Homogenous
	Smooth, Buttery & Homogenous
	Smooth, Buttery & Homogenous
	Visual

	9
	Base oil Viscosity (KV@40(C) ,cSt
	130 - 160
	130 - 160
	200 - 230
	ASTM D 445

	10
	Base Oil Type
	Mineral
	Mineral
	Mineral
	

	11
	Oil separation

 40(C for 168 Hours

 (% loss)
	6 Max
	6 Max
	6 Max
	IS 1448 [P 85]

	12
	Oil separation

 100(C for 30 Hours

 (% loss)
	6 Max
	6 Max
	6 Max
	IS 1448 [P 89]

	13
	Resistance to water washout

 (% loss)
	6 Max
	6 Max
	6 Max
	ASTM D 1264

	14
	Copper corrosion
	1b Max
	1b Max
	1b Max
	ASTM D 4048

	15
	Roll Stability
16 Hours (%)
	<25
	<25
	<25
	ASTM D 1831

	17
	4 Ball Weld Load (Kg)(Min)
	250 
	250 
	315
	ASTM D 2596

	18
	4 Ball Wear Scar (mm)
	0.6 Max
	0.6 Max
	0.6 Max
	ASTM D 2266

	19
	EMCOR Rust Test
	0,0
	0,0
	0,0
	IP 220/93

	20
	Operating Range (℃)
	-20℃ to +130
	-20℃ to +130
	-20℃ to +130
	


     










         Page 2 of 3

                  Lithium EP Greases NLGI 1, 0, 00


	Sr.No.
	Test
	Control Range/Limit

EP1
	Control Range/Limit

EP0
	Control Range/Limit

EP00
	Test Method

	1
	Penetration:
	
	
	
	ASTM D 217-02

	
	 Work 60X
	310 – 340
	355 – 385
	400 – 430
	

	
	Typical
	325
	370
	415
	

	2
	Work 100,000X
	+30 Max 

(from Work 60X)
	+30 Max 

(from Work 60X)
	+30 Max

(from Work 60X)
	ASTM D 217

	3
	NLGI Grade
	1
	0
	00
	

	4
	Drop Point ((C)
	>185
	>180
	>170
	ASTM D 566

	5
	  Rust Preventive Characteristic
	Pass
	Pass
	Pass
	ASTM D 1743

	6
	Colour
	Golden Brown
	Golden Brown
	Golden Brown
	Visual

	7
	Soap
	Lithium
	Lithium
	Lithium
	

	8
	Appearance
	Smooth, Buttery & Homogenous
	Smooth, Buttery & Homogenous
	Smooth, Buttery & Homogenous
	Visual

	9
	Base oil Viscosity (KV@40(C) ,cSt
	130 - 160
	130 - 160
	130 - 160
	ASTM D 445

	10
	Base Oil Type
	Mineral
	Mineral
	Mineral
	

	11
	Copper corrosion
	1b Max
	1b Max
	1b Max
	ASTM D 4048

	12
	Roll Stability
16 Hours (%)
	<25
	<25
	<25
	ASTM D 1831

	13
	4 Ball Weld Load (Kg)(Min)
	250 
	250 
	250
	ASTM D 2596

	14
	4 Ball Wear Scar (mm)
	0.6 Max
	0.6 Max
	0.6 Max
	ASTM D 2266

	15
	EMCOR Rust Test
	0,0
	0,0
	0,0
	IP 220/93

	16
	Operating Range (℃)
	-20℃ to +130
	-20℃ to +130
	-20℃ to +130
	













    Page 3 of 3
    TURBHE CHEMICALS PVT. LTD.








